CD-fungi, fungus, biodeterioration, tropic

Research in progress. Consejo Superior de Investigaciones Científicas. Madrid. Spain. This is an advertisement to CD’s collectors,

which have destroyed CDs by fungi, mainly from tropical areas

THE SPANISH TEAM, WHICH IS ANALYZING THE CD-FUNGI NEEDS MORE SAMPLES OF BIODETERIORED CDs,

please contact to: Javier Garcia Guinea  guinea@mncn.csic.es

Museo Nacional Ciencias Naturales.  C/ José Gutiérrez Abascal 2

Madrid 28006 Spain     tf 00 34 91 4111328 ext 1190

-------additional information in the scientific paper----------

SUBMITTED PAPER TO NATURWISSENSCHAFTEN:

Growing of Fungal Bioturbation Paths in a Compact Disk

Javier Garcia-Guinea, Victor Cardenes,

Museo Nacional de Ciencias Naturales, CSIC

C/ Jose Gutierrez Abascal 2, 28006-Madrid, Spain

Fax +34 91 5644740  Tel: + 34 91 4111328 (ext 1190)

Correspondence author: E-mail: guinea@mncn.csic.es

## Angel Tomás Martinez, Maria Jesus Martinez

Centro de Investigaciones Biológicas, CSIC
C/ Velázquez 144, 28006-Madrid, Spain.

Fax: +34 91 562 75 18  Tel: +34 91 561 18 00 (ext 4407)

ABSTRACT.- We report here on bioturbation traces, with micro-dendrite textures, composed of a mixture of altered aluminum and polycarbonate, which have been developed in a common compact disc (CD) destroying information pits. Fungal hyphae proliferated in these deteriorated zones, and Geotrichum-type fungus was isolated from surface-sterilised CD fragments. The severe biodeterioration described is attributed to the slow growth of this arthroconidial fungus on the CD material in the tropical indoor environment of Belize, Central America (~30ºC, ~90% humidity).